## Slide 1
F-TM-001 rev A
Your
Presenter:
Gary Barone
Gary is SilcoTek’s Business Unit Manager in charge of sales, marketing, and engineering efforts.
Today, he will give you expert tips and best practices for proper care and maintenance of SilcoTek-coated products, helping you achieve peak performance for longer usable life.
Welcome to the Webinar!
A Step-by-Step Guide to SilcoTek® Coating Care
We will begin 2 minutes past the hour

## Slide 2: Welcome!
Webinar will be recorded and emailed to you
  You can find it any time on SilcoTek.com
?
#AskSilcoTek on Twitter (@SilcoTek)
Send questions via message bar

## Slide 3: What We’ll Cover
A general overview inspection and proper cleaning techniques
Application-specific tips
Do’s and don’ts of SilcoTek coating care

## Slide 4: Your Presenter: Gary Barone
B.S. Chemical Engineering; MBA
R&D with Restek since ’90
Been working on coatings since ’94 from R&D/Tech. Service/Marketing/Sales

## Slide 5: Introduction
SilcoTek coatings are rugged, durable and are used in a lot of applications
Performance will be impacted by contamination and poor environment
Good news: Performance can be maintained if not completely restored

## Slide 6: Coating Care Tips

## Slide 7: Can I bend the coating?
Yes – SilcoTek coatings can be flexed without cracking or flaking
Be careful not to expose new, uncoated surface area (especially in analytical applications)
Minimum bend radius of 16x OD of tubing is recommended

## Slide 8: Flexibility Demo Video
Notes: Tube bending video

## Slide 9: Nuts and Ferrules
Nuts and ferrules should not be coated
Nuts are not in the flow path, coated ferrules have potential to leak
A proper connection will ensure minimal active surface area on ferrules

## Slide 10: Welding
SilcoTek can produce a good coating on TIG and MIG welds, or vacuum nickel brazes
Welding after coating will remove the coating ~4mm from the heat affected zone

## Slide 11: Do’s and Don’ts of SilcoTek Coating Care

## Slide 12: Do’s and Don’ts
Don’t use basic solutions or soaps with pH > 8
  SilcoNert, Silcolloy, etc. will be damaged
  Dursan OK with bases, should still avoid

## Slide 13: Do’s and Don’ts
Do clean as part of regular maintenance
  Contaminants can accumulate and lead to issues, especially in analytical applications

## Slide 14: Do’s and Don’ts
Don’t steam clean a Silco- coating
  Layer is not physically destroyed, but surface chemistry changes
  Steam cleaning will drastically reduce inertness to active compounds

## Slide 15: Do’s and Don’ts
Do send your treated parts in for re-coating as needed
  We can strip the old coating, deposit a fresh one, and get your used parts back to peak performance without replacement

## Slide 16: Do’s and Don’ts
Don’t abrade a SilcoTek coating
  A Scotch-Brite™ pad with light hand pressure will remove Silco-coatings
  Dursan is abrasion resistant, but still use caution

## Slide 17: Do’s and Don’ts
Don’t let connections gall
  Coated-on-coated connections can gall, or “cold weld,” parts together
  Use PTFE tape or simply remove the coating from one of the threads

## Slide 18: When to Clean

## Slide 19: Some Indicators
Visual inspection clues
Declining/Poor analytical results
Process Upset in stream being sampled
Sitting on the shelf

## Slide 20: Visual: The “rainbow?”
Color is indicative of thickness
  Like oil on water
Colors can vary substantially even at nano-scale thickness variation

## Slide 21: What if there’s no rainbow?
Is the coating the thick Silcolloy?
  If not, possible loss of coating
  Or if Dursan, it can visibly change during oil contamination
Change in appearance over time or vs new parts?
  Visible Buildup tars/particles inside vs. outside?
  Is one end different? Dark vs. light? Matte vs. glossy?
Localized areas of loss due to corrosion or wear?

## Slide 22: Disappearing Coating

## Slide 23: Cleaning 101

## Slide 24: Why and How to Clean
Often used in field or process
Build up of inorganics and heavy organics cause problems
The SilcoTek coated components can be “new” again

## Slide 25: Cleaning Tips
Rinse with a solvent that will dissolve contaminants from the application
  Nonpolar solvent for hydrocarbons
  Polar solvent for more active contaminants

## Slide 26: Cleaning Tips
Mild sonication is okay, but don’t over-sonicate
  Solids can be removed with a soft nylon bristle brush using light pressure

## Slide 27: Sonication Video

## Slide 28: Cleaning Tips
Water based cleaning system
  Use Neutral pH surfactants and detergents
  Know what’s in off the shelf cleaners
  Mild acidic cleaning at room temperature (except HF)
Do not use basic solutions or soaps with pH>8! rule

## Slide 29: Cleaning Tips
Do not steam clean any SilcoTek-treated components!

## Slide 30: Cleaning Tips
Commonly recommended solvents
  Acetone
  Methanol/IPA
  Dichloromethane
  Water for inorganics and particulate

## Slide 31: Application-Specific Tips

## Slide 32: Every Challenge is different
Largest application uses:
  Laboratory/Medical test equipment
  Petro/Refining
  Natural Gas/LNG
  Stack Gas Sampling/CEMS
  Semiconductor

## Slide 33: Laboratory Equipment
Chromatographs, Diagnostic equipment
  Often clean environment
  non-volatiles or heavy organic buildup
Bake and purge with Nitrogen.
Solvent cleaning great for renewing

## Slide 34: Petro/Refining
Sampling equipment and process analyzers
  Heavy organics a problem
  Particulate a problem
  Upsets, could be anything

## Slide 35: Petro/Refining
Use coated particulate filters!
Solvent cleaning, if can be done
If you get water use IPA, Acetone.
Do NOT use plant steam!

## Slide 36: Natural Gas/LNG
Pipeline probes, sample cylinders, transfer tubing
Largest challenge is moisture and particulate
If samples taken near wall of pipeline, all kinds of possible contamination

## Slide 37: Natural Gas/LNG
Use Filters!
  Particulate
  Water drop outs
If sample probes are showing particulate
  wipe off with solvents
  run through soft brushes with solvent
Water contamination; IPA, Acetone

## Slide 38: Stack/CEMS
Very tough environment
  Hot, acidic exhaust gases
  Massive soot and particulate
Use filtration systems
Particulate can be cleaned from probes through wiping and soft brushing

## Slide 39: Stack/CEMS
Inspect for corrosion
Inspect for coating loss
Primary attack areas will be outside of stack probe
If coating loss identified, re-coat

## Slide 40: Semiconductor
Very clean environment, too clean
May require pre-install cleaning
Trace particulate possible
Source SemiCon approved Cleaning firms. Make sure they know the Do’s and Don’ts

## Slide 41: Conclusion
Coatings will last a long time
Every application different, what is unique about yours?
Clean the dirt coating off the coating!
Measure of last resort, re-coat

## Slide 42: Questions? Submit via the Webinar app., #AskSilcoTek on Twitter, or by emailing SilcoD@SilcoTek.com

## Slide 43: Thank you!
E: SilcoD@SilcoTek.com | P: +1 (814) 353-1778
www.SilcoTek.com